Technical Data Sheet

(TDS)

| Product information |  |  |  |  |
| --- | --- | --- | --- | --- |
| Product Name | : | Redispersible Polymer Powder (RDP/VAE) |  |  |
| Product application | ： | RDP (TR-680R) Redispersible polymer powder is a water-soluble redispersible powder, a vinyl acetate-ethylene polymer, suitable for outdoor plastering mortar and exterior walls flexible putty. Advantages: 1. Improve the impact resistance, durability and wear resistance. 2. Improve the bonding strength and cohesion. 3. Improve the weather resistance and freeze-thaw resistance and prevent mortar cracking. 4. Improve the hydrophobicity and reduce water absorption. 5. Improve the bending strength and flexural strength. Application range: 1. Flexible putty for exterior walls 2. Lacquer primer putty 3. Anti-crack plaster putty 4. Tile adhesive 5. Exterior wall external insulating plastering mortar |  |  |
| Technical Specification |  |  |  |  |
| Appearance | : | White or off white flowable powder |  |  |
| Odor | : | Weak odor |  |  |
| Model |  | TR-680R |  |  |
| Composition | : | Vinyl acetate, ethene polymer |  | 99.2% |
| Test items |  | Standard requirement | Test result | evaluate |
| Exterior |  | No color difference,impurities, agglomeration |  | qualified |
| Bulk density, kg/m3 |  | 550±50 | 525 | qualified |
| Content,% |  | ≥98.0 | 99.4 | qualified |
| PH |  | 5~9 | 7.5 | qualified |
| Ash |  | 12±2 | 12.6 | qualified |
| Tg |  | -9℃ | -9℃ | qualified |
| MFFT |  | 0℃ | 0℃ | qualified |
| Storage Information |  |  |  |  |
| Storage Temperature(°C) and condition | : | Room temperature, cool and dry place. |  |  |
| Transport Information |  |  |  |  |
| Marine Pollutant | : | No |  |  |
| ADR/RID | : | Not Dangerous Goods |  |  |
| IMDG | : | Not Dangerous Goods |  |  |
| IATA | : | Not Dangerous Goods |  |  |
|  |  | Taian Tianrun Gome New Material Co., Ltd. Add: Feicheng City, Taian City, Shandong Province,China Contact: Leo Liu MOB/WA: +86 18905481653 Email: leo@rdptianrun.com |  |  |