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Technical Data Sheet
(TDS)
	Product information
	
	

	Product Name
	:
	Redispersible Polymer Powder (RDP/VAE)

	Product application
	：
	[bookmark: OLE_LINK2]RDP (TR-680R) Redispersible polymer powder is a water-soluble redispersible powder, a vinyl acetate-ethylene polymer, suitable for outdoor plastering mortar and exterior walls flexible putty.
Advantages:
1. Improve the impact resistance, durability and wear resistance.
2. Improve the bonding strength and cohesion.
3. Improve the weather resistance and freeze-thaw resistance and prevent mortar cracking.
4. Improve the hydrophobicity and reduce water absorption.
5. Improve the bending strength and flexural strength.
[bookmark: OLE_LINK1]Application range:
1. Flexible putty for exterior walls
2. Lacquer primer putty
3. Anti-crack plaster putty
4. Tile adhesive
5. Exterior wall external insulating plastering mortar

	Technical Specification
	
	

	Appearance
	:
	White or off white flowable powder

	Odor
	:
	Weak odor

	Model
	
	TR-680R

	Composition
	:
	Vinyl acetate, ethene polymer
	99.2%

	Test items
	
	Standard requirement
	Test result
	evaluate

	Exterior
	
	No color difference,impurities, agglomeration
	qualified

	Bulk density, kg/m3
	
	550±50
	525
	qualified

	Content,%
	
	≥98.0
	99.4
	qualified

	PH
	
	5~9
	7.5
	qualified

	Ash
	
	12±2
	12.6
	qualified

	Tg
	
	-9℃
	-9℃
	qualified

	MFFT
	
	0℃
	0℃
	qualified

	Storage Information
	
	
	

	Storage Temperature(°C) and condition
	:
	Room temperature, cool and dry place. 

	Transport Information
	
	

	Marine Pollutant
	:
	No

	ADR/RID
	:
	Not Dangerous Goods

	IMDG
	:
	Not Dangerous Goods

	IATA
	:
	Not Dangerous Goods
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