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	Product information
	
	

	Product Name
	
	Polycarboxylate Superplasticizer

	Product application
	
	Polycarboxylate Superplasticizer is a kind of high performance superplasticizer powder , produced by high-speed centrifugal spray drying process.

	Technical Specification
	
	

	Appearance
	
	White powder

	Bulk density（kg/m³）
	
	600±100

	PH(20% aqueous solution)
	
	7.0-9.0

	Moisture content
	
	≤3

	Rate of water reduction
	
	≥25

	Water reduction rate 
recommended dosage (accounted for gel material %)
	
	0.2-0.4

	Purity
	
	95.5%

	Application Environment
	
	

	[bookmark: OLE_LINK1]1.self-leveling mortar

	2.common grout

	3.repair mortar

	4.floor mortar

	5.reagents for high performance concrete

	6.high strength concrete 

	7.large flow concrete

	8.gypsum plastering

	Advantage

	(1) Low dosage and high water reduction rate

	(2) Good fluidity retention of concrete mixture; 

	(3) Good compatibility with cement;

	(4) The prepared concrete has a small shrinkage, which is conducive to improving the volume stability and durability of concrete; 

	(5) Environmental protection and pollution-free during production and use, belonging to green admixture

	Storage Information and Packaging

	Stored in the dry environment with temperature below
30°C
Do not store product for more than six months,if warranty
period is beyond and no caking phenomenon exists,it can
still be used
After being opened,the powder not used up shall be
sealed to avoid being affected with damp because of air
contact
25kg/bag or custom packaging
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	Taian Tianrun Gome New Material Co., Ltd.
Add: Feicheng City, Taian City, Shandong Province,China
Contact: Leo Liu
MOB/WA: +86 18905481653
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