Technical Data Sheet (TR-5088)

(TDS)

| Product information |  |  |
| --- | --- | --- |
| Product Name |  | Polycarboxylate Superplasticizer |
| Product application |  | Polycarboxylate Superplasticizer is a kind of high performance superplasticizer powder , produced by high-speed centrifugal spray drying process. |
| Technical Specification |  |  |
| Appearance |  | White powder |
| Bulk density（kg/m³） |  | 600±100 |
| PH(20% aqueous solution) |  | 7.0-9.0 |
| Moisture content |  | ≤3 |
| Rate of water reduction |  | ≥25 |
| Water reduction rate recommended dosage (accounted for gel material %) |  | 0.2-0.4 |
| Purity |  | 95.5% |
| Application Environment |  |  |
| 1.self-leveling mortar |  |  |
| 2.common grout |  |  |
| 3.repair mortar |  |  |
| 4.floor mortar |  |  |
| 5.reagents for high performance concrete |  |  |
| 6.high strength concrete |  |  |
| 7.large flow concrete |  |  |
| 8.gypsum plastering |  |  |
| Advantage |  |  |
| (1) Low dosage and high water reduction rate |  |  |
| (2) Good fluidity retention of concrete mixture; |  |  |
| (3) Good compatibility with cement; |  |  |
| (4) The prepared concrete has a small shrinkage, which is conducive to improving the volume stability and durability of concrete; |  |  |
| (5) Environmental protection and pollution-free during production and use, belonging to green admixture |  |  |
| Storage Information and Packaging |  |  |
| Stored in the dry environment with temperature below 30°C Do not store product for more than six months,if warranty period is beyond and no caking phenomenon exists,it can still be used After being opened,the powder not used up shall be sealed to avoid being affected with damp because of air contact 25kg/bag or custom packaging |  |  |
|  |  | Taian Tianrun Gome New Material Co., Ltd. Add: Feicheng City, Taian City, Shandong Province,China Contact: Leo Liu MOB/WA: +86 18905481653 Email: leo@rdptianrun.com |